PAVING SCHEDULE:

| TYPE | DESCRIPTION | PATTERN | MODULE | THICKNESS | BASE | INTEGRAL COLOR | SAND (WCS) | COARSE AGGREGATE | CEMENT | Lithocrete( Aggregate | FINISH | JOINT WIDTH | REBAR | REMARKS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | Lithocrete( Concrete Paving | Square | ?” x ?” | 4” | 4” ABC | Davis San Diego Buff | Salt River | ½” Salt River Aggregate | Gray Type II or equal | Rosso Nero | LithocreteTM | 1/8” | #3 at 18”o.c.e.w. | Lithocrete( is a patented paving process – match Progressive Hardscapes sample #00-XX. |

PAVING SCHEDULE NOTES:

1.	Verify layout of concrete paving indicated on Drawings and indicated on this paving schedule prior to starting Work.  Contact Owner's Authorized Representative once paving forms have been laid out for review and approval.

2.	Lithocrete( architectural concrete paving is installed under U.S. patents #4,748,788 and 6,016,635.  Contact Progressive Hardscapes, LLC. authorized Lithocrete( contractor at (623) 582-2274 or mike@ProgressiveHardscapes.com

for a list of licensed Lithocrete( installers in the project’s area www.lithocrete.com.

3.	Refer to Specification – Lithocrete( Architectural Concrete Paving for additional paving information.

4.	Construct paving indicated on this schedule per approved mock-ups.

5.	Do not allow sawcut jointing to deviate more than (+/-) 1/16-inch overall in a 10-foot run.  Of primary importance is that sawcutting is to be cut straight.

6.	Construct paving mock-ups on-site for paving types described in this paving schedule for Owner’s Authorized Representative review and approval.  Approved samples are to remain on-site in an accessible location throughout duration of project.  Approved samples will to be basis for future paving work.